- Приложение № 1А

- ТЕХНИЧЕСКИ  ПАРАМЕТРИ  НА  ЗАГОТОВКИТЕ  ЗА  БЪЛГАРСКИ  РАЗМЕННИ  МОНЕТИ

- С КУПЮРИ 1, 2 И 5 СТОТИНКИ, ЕМИСИЯ 2000 ГОДИНА

Радиус на закръгление (Bр.з.) 3.00 мм.

| Купюр | Диаметър на неренделована заготовка ± 0.02 мм D н. к p. | Диаметър на ренделована заготовка ± 0.05мм D p.з. | Радиус на закръгление на ренделована повърхнина Bp.з. | Материал | Тегло на заготовката | Твърдост на заготовка по Викерс |
| --- | --- | --- | --- | --- | --- | --- |
|  | мм. | мм. | мм. |  | грама |  |
| 1 ст. | 16.00 | 15.80 | 3 | Fe/галванизирана; цвят – златист | 1.8 ± 0.08 | 80–100 HV/10/30s |
| 2 ст. | 18.00 | 17.80 | 3 | Fe/галванизирана; цвят – златист | 2.5 ± 0.11 | 80–100 HV/10/30s |
| 5 ст. | 20.00 | 19.80 | 3 | Fe/галванизирана цвят – златист | 3.5 ± 0.15 | 80–100 HV/10/30s |

Контролирани параметри посредством машина Visia Compact на фирма „Proditec”:

- Отклонение от размер и форма по диаметър;

- Нахапани заготовки и полукръгчета;

- Неренделовани заготовки;

- Отклонение по дебелина на заготовката;

- Отклонение в тегло;

- Контрол по лицевата и обратната повърхнина на заготовките по предоставени еталонни (мостри) заготовки за:

- Разноцветност, по предоставени еталонни заготовки и сравняване с тях;

- Тъмни и светли петна, точки, пъпки и негалванизирани участъци;

- Подбитости , дълбоки драскотини чрез сравняване с еталонни заготовки по повърхнината;

- Подбитости и неренделовани участъци по канта.

Химичен състав:

Стомана по евро стандарт EN 10139 (БДС EN 10139:2000) с електролитно покритие първи слой: мед (Cu)
с дебелина 12 микрона и втори слой електролитно покритие от бронз (CuSn8) с дебелина 12 микрона. Обща дебелина на покритието 24 микрона.

- Appendix No. 1А

- Technical specifications of the coin blanks for Bulgarian circulation coins

- of 1, 2 and 5 stotinki denominations, issue 2000

Rounding on the edge (Bр.з.) 3.00 mm

| Denomination | Diameter of a non-rimmed coin blank ± 0.02 мм D н. кp. | Diameter of a rimmed coin blank ± 0.05мм D p.з. | Rounding on the edge of the rimmed surface Bp.з. | Material | Weight of a coin blank | Hardness of a coin blank by Vickers |
| --- | --- | --- | --- | --- | --- | --- |
|  | mm | mm | mm |  | grams |  |
| 1 st. | 16.00 | 15.80 | 3 | Fe/electroplated; colour – golden | 1.8 ± 0.08 | 80–100 HV/10/30s |
| 2 st. | 18.00 | 17.80 | 3 | Fe/electroplated; colour – golden | 2.5 ± 0.11 | 80–100 HV/10/30s |
| 5 st. | 20.00 | 19.80 | 3 | Fe/electroplated; colour – golden | 3.5 ± 0.15 | 80–100 HV/10/30s |

Parameters controlled by a Visia Compact machine of the Proditec Company:

- Deviations from the size and form by diameter;

- Bitten coin blanks and semicircles;

- Non-rimmed coin blanks;

- Deviations in the thickness of the coin blank;

- Deviations in the weight;

- Control over the obverse and reverse surface of the coins blanks by the provided standard (sample) coin blanks with regard to:

- Difference in colour, by comparison with the provided standard coin blanks;

- Dark and lighter spots, dots, protrusions and non-electroplated areas;

- Dents, deep scratches by comparing the surface with the standard coin blanks;

- Dents and non-rimmed areas along the edge.

Chemical composition:

Steel according to the European standard EN 10139 (BDS EN 10139:2000), electroplated; first coating of copper plating (Cu), 12 microns thick; and second coating of bronze plating (CuSn8), 12 microns thick. Total thickness of electroplating - 24 microns.